XHD 12

Heavy Port & Airport

12” (305mm) ID Trench Forming System

Standard Specifications

System ID#: TR12-12.502G.JB-J22G

Manufactured by ABT, Inc., 259 Murdock Road, Troutman, NC – (800) 438-6057.  www.abtdrains.com

System Components:

Forms-TR12: Pre-manufactured trench forms using recyclable non-CFC EPS foam. Forms to be pre-sloped or non-sloped form segments with each segment 12” (305mm) wide.  Non-sloping sections must have written approval by engineer prior to installation. Forms to have radius bottom and 15.75” (400mm) grate seat width. Forms to be within 1/16” (1.5mm) tolerances. Invert slope is per application requirement as noted on plans. Formwork assembly must be prevented from floating during concrete placement without penetrating the sub grade. Formwork to be anchored to the earth using steel no-float legs and an anchor slab pour. Tie wires that assure constant frame spacing and grate seat dimension to be provided. Non-petroleum based form release is to be used for smooth interior walls and easy form removal.

Grating-12.502G.JB: Uncoated ductile iron conforming to ASTM A 536-84 with a minimum inlet area of 0.79ft2/Lft (0.24m2/Lm). Grates shall meet a minimum vertical proof load of 2496 psi (200,000 lbs) by utilizing a 9” x 9” centered contact area without failure. Grates shall comply with all the requirements of FAA Specification AC 150/5320-6E, Appendix 3. Grating shall be made in USA, and shall conform to the “Buy American Act” if Federal Aid finances apply.

Frames-J22G: Post fabrication hot dipped galvanized 3.0” x 3.0” x .31” (76.2mm x 76.2mm x 7.93mm) steel angle frames conforming to ASTM A36. Galvanizing to conform to ASTM A123-89a. Standard headed concrete anchor studs bisect grate retainer anchor lugs providing a frame-anchoring device every 9.84” (250mm). Grate frames to provide a minimum of 2.25 square inches concrete bearing area with 5.25 square inches of concrete contact per inch of trench length on each side. Grates are retained non-rigidly at all corners. Non-threaded removable .5” Stainless Steel pins located on 3.28ft (1.0M) centers along the frames bisected by .5” non-removable grate retaining device on 3.28ft (1.0M) centers. Grate retainer performance shall not degrade with service loads or thermal cycling. Frames and retainers shall be made in USA, and shall conform to the “Buy American Act” if Federal Aid finances apply.

Quality Assurance:

Submittals: A Certificate of Compliance in conformance with the provisions of these Standard Specifications shall be furnished to the Engineer. Grates shall be independently tested.

Post Construction Inspection - Formwork is to be fully removed, without exception, to allow for inspection and if needed repair of any voids and or concrete consolidation issues below the frame, trench walls and invert. Grate and grate retainer inspection shall be performed to ensure that all grates and retainers are installed and are properly seated in place.